Hands-on: Advanced functionals
Iurii Timrov
Theory and Simulation of Materials (THEOS), and National Centre for Computational Design and Discovery of Novel Materials (MARVEL),
École Polytechnique Fédérale de Lausanne (EPFL), Lausanne, Switzerland
Summer School on Advanced Materials and Molecular Modelling with Quantum ESPRESSO
Ljubljana, Slovenia
17 September 2019

---
Outline
Exercise 1: DFT+U study of FeO
Exercise 2: DFT with hybrid functionals: study of Si
Exercise 3: DFT with Van der Waals functionals: study of graphite

---
Outline
Exercise 1: DFT+U study of FeO
Exercise 2: DFT with hybrid functionals: study of Si
Exercise 3: DFT with Van der Waals functionals: study of graphite

---
DFT+U
The DFT+U total energy:
The Hubbard correction energy:
effective Hubbard
      parameter
The occupation matrix:
The total occupation of localized states (d or f) at site I :
The Kohn-Sham equation:

---
Localized-states manifold
How do we know to what states of a Hubbard atom the Ueff correction will be applied?
Currently, this is hard-coded (in Quantum ESPRESSO 6.4.1)
Check two subroutines in quantum-espresso/Modules :
set_hubbard_n.f90
set_hubbard_l.f90
principal quantum number “n”
orbital quantum number “l”
For Fe : n = 3
For Fe : l = 2
Apply the Hubbard Ueff correction to the 3d electrons of Fe

---
Input file pw.FeO.scf.in
SCF calculation
Experimental lattice parameter
'MV' smearing for metals (FeO is metallic @PBEsol)
Spin-polarized (collinear) calculation
(antiferromagnetic ordering)
Initialize Hubbard parameters for two types of Fe
Two sublattices of Fe atoms
O
Fe

---
Input file pw.FeO.nscf.in
NSCF calculation
NSCF input is very similar to the SCF input,
     but there a few differences which are
        highlighted here
Number of electronic bands
Projected DOS must be converged with respect to
the number of k points. Also, number of bands must
be large enough, to have converged projected DOS
in a specific energy range. All this is controlled here.
k points mesh which is denser than in SCF

---
Input file projwfc.FeO.in
Simple Gaussian broadening of PDOS
Value of Gaussian broadening, in Ry (not eV!)
Minimum and maximum value of energy for the plot, in eV
Energy grid step
Gnuplot script: plot_pdos.gnu
Inspect the script: it aims at plotting Fe-3d state (majority spin and minority spin)
and O-2p states.
PDOS is shifted such that the Fermi energy corresponds to the zero of energy.
Visualize the file “FeO_PDOS.eps”

---
PDOS of FeO from standard DFT calculation
DFT predicts FeO to be metallic (but this is wrong!)
Let's try DFT+U
Experimentally FeO is know to be insulating

---
Input file pw.FeO.scf.in for DFT+U
Here we want to put a Hubbard U correction for
        3d electrons of Fe atoms
Which value of U to use?
For every material Hubbard U is different; here we use
U = 5.2 eV for Fe-3d states for demonstration purposes
Hubbard U values (in eV) for atomic type 1 & type 2
Hubbard U can be computed from first principles:
I. Timrov, N. Marzari, M. Cococcioni, PRB 98, 085127 (2018)

---
DFT vs DFT+U
DFT
DFT+U
The solution with DFT is metallic
The solution with DFT+U is also metallic...
The 3d states of Fe a fully occupied for the majority spin, while for the minority spin they are still partially occupied.
The reason of this failure of DFT+U is that it gets stuck in a local minimum (which corres- ponds to a metallic state) and it needs a “hint” to reach the correct (insulating) ground state.

---
How to “push” DFT+U to the global minimum?
Check the output file pw.FeO.scf.out from the DFT+U calculation
After the 1-st iteration we have:
Fe1
Fe2

---
How to “push” DFT+U to the global minimum?
Check the output file pw.FeO.scf.out from the DFT+U calculation
After the 1-st iteration we have:
Fe1
starting_ns_eigenvalue(5,2,1)= 1.0
Fe2
starting_ns_eigenvalue(5,1,2)= 1.0
Let's try to force/suggest the occupancy of the 5-th state to be 1.0 instead of 0.296 !
Why 5-th state? Because it is the one which is non-degenerate and if occupied fully could lead
to an insulating result.

---
A “hint” for DFT+U where to look for a correct solution
starting_ns_eigenvalue(m,ispin,ityp)
In the first iteration of a DFT+U run it overwrites the
m-th eigenvalue of the ns occupation matrix for the
ispin spin-component of atomic species of type ityp.
Why? This is useful to suggest the desired orbital occu-
pations when the default choice takes another path.
   fully
occupied
spin 2 (down)
type 1: Fe1
5-th eigenvalue
starting_ns_eigenvalue(5,2,1)= 1.0
starting_ns_eigenvalue(5,1,2)= 1.0
   fully
occupied
spin 1 (up)
type 2: Fe2
5-th eigenvalue

---
Understanding the setup of starting_ns_eigenvalue
Check the output file pw.FeO.scf.out from the DFT+U calculation (with starting_ns_eigenvalue):
After the 1-st iteration (i.e. when we forced the 1.0 occupancy of the 5-th state) we have:
Fe1
After this the DFT+U calculation converges to an insulating ground state with lower energy
than the previous one.

---
Comparison of DFT+U results w/o and w/ starting_ns_eigenvalue
DFT+U
DFT+U (with starting_ns_eigenvalue)
The solution with DFT+U is insulating
The solution with DFT+U is metallic
Agreement with the experiement!

---
Outline
Exercise 1: DFT+U study of FeO
Exercise 2: DFT with hybrid functionals: study of Si
Exercise 3: DFT with Van der Waals functionals: study of graphite

---
Input file pw.Si.scf.in
SCF calculation
Override the functional written in the PP file.
Important: use a PP for the closest GGA (PBE
In this case), there are no PP's for hybrids.
Grid for the q points
1x1x1 0s the minimal grid (q=0), it is fast
but not very accurate
If .true. Use extrapolation for the q->0 limit
Specifies that the singularity at q->0 is
analytically integrated

---
Popular hybrid functionals
input_dft = “pbe0”
J.P.Perdew, M. Ernzerhof, K.Burke, JCP 105, 9982 (1996)
C. Adamo, V. Barone, JCP 110, 6158 (1999)
input_dft = “b3lyp”
 P.J. Stephens,F.J. Devlin,C.F. Chabalowski,M.J. Frisch, J.Phys.Chem 98, 11623 (1994)
input_dft = “hse”
Heyd, Scuseria, Ernzerhof, J. Chem. Phys. 118, 8207 (2003)
Heyd, Scuseria, Ernzerhof, J. Chem. Phys. 124, 219906 (2006)

---
Types of treatement of divergences at q->0

---
Convergence of the total energy
wrt q point grid

---
Outline
Exercise 1: DFT+U study of FeO
Exercise 2: DFT with hybrid functionals: study of Si
Exercise 3: DFT with Van der Waals functionals: study of graphite

---
Graphite
Graphite has Van der Waals (dispersive) interactions between layers.
The equilibrium inter-layer distance is too small with LDA, and too large with GGA
        with respect to the experimental value (3.336 A).
Van der Waals interactions must be taken into account.

---
Input file pw.graphite.scf.in
SCF calculation
Calculation of forces and stress
Hexagonal lattice, a and c are in Angtrom!
Override the functional written in the PP file.
Important: use PP for the closest GGA (PBE in
this case), because there are no PP for non-
local functionals
Remember to generate and store the kernel table!
        vdW_kernel_table
The k point grid is denser along xy than along z,
reflecting shorter periodicity in the xy plane

---
Input file pw.graphite.vc-relax.in
Variable-cell optimization
Variable-cell optimization
If we do not specify anything inside these namelists,
then the default values will be used for various
control parameters

---
Structural optimization in graphite