QE-2021: Hands-on session – Day-4
Advanced functionals
Iurii Timrov (EPFL, Switzerland)

---
Outline
Example 1: DFT+U study of FeO
Example 2: DFT with hybrid functionals: study of Si
Example 3: DFT with Van der Waals functionals: study of graphite
(We will use HPC for this hands-on, because the examples are quite heavy)

---
Outline
Example 1: DFT+U study of FeO
Example 2: DFT with hybrid functionals: study of Si
Example 3: DFT with Van der Waals functionals: study of graphite

---
DFT+U
The DFT+U total energy:
The Hubbard correction energy:
effective Hubbard
      parameter
The occupation matrix:
The total occupation of localized states (d or f) at site I :
The Kohn-Sham equation:

---
Localized-states manifold
How do we know to what states of a Hubbard atom the Ueff correction will be applied?
Currently, this is hard-coded (in Quantum ESPRESSO 6.7)
Check two subroutines in quantum-espresso/Modules :
set_hubbard_n.f90
set_hubbard_l.f90
principal quantum number “n”
orbital quantum number “l”
For Fe : n = 3
For Fe : l = 2
Apply the Hubbard Ueff correction to the 3d electrons of Fe

---
Input file pw.FeO.scf.in
SCF calculation
!
ESPRESSO_PSEUDO and ESPRESSO_TMPDIR
!
Experimental lattice parameter
'MV' smearing for metals (FeO is metallic @PBEsol)
Spin-polarized (collinear) calculation
(antiferromagnetic ordering)
Initialize Hubbard parameters for two types of Fe
Two sublattices of Fe atoms
O
Fe

---
Input file pw.FeO.nscf.in
NSCF calculation
!
!
NSCF input is very similar to the SCF input,
 but there are a few differences which are
        highlighted here
Number of electronic bands
Projected DOS must be converged with respect to
the number of k points. Also, number of bands must
be large enough, to have converged projected DOS
in a specific energy range. All this is controlled here.
k points mesh which is denser than in SCF

---
Input file projwfc.FeO.in
!
Simple Gaussian broadening of PDOS
Value of Gaussian broadening, in Ry (not eV!)
Minimum and maximum value of energy for the plot, in eV
Energy grid step
Gnuplot script: plot_pdos.gp
Inspect the script: it aims at plotting Fe-3d state (majority spin and minority spin)
and O-2p states.
PDOS is shifted such that the Fermi energy corresponds to the zero of energy.
Visualize the file “FeO_PDOS.eps”

---
PDOS of FeO from standard DFT calculation
DFT predicts FeO to be metallic (but this is wrong!)
Let's try DFT+U
Experimentally FeO is know to be insulating

---
Input file pw.FeO.scf.in for DFT+U
Here we want to put a Hubbard U correction for
        3d electrons of Fe atoms
!
!
Which value of U to use?
For every material Hubbard U is different; here we use
U = 4.6 eV for Fe-3d states (see next slides)
Hubbard U values (in eV) for atomic type 1 & type 2

---
DFT vs DFT+U
DFT+U
DFT
The solution with DFT+U is insulating
The solution with DFT+U is metallic
Agreement with the experiement!

---
How to compute the Hubbard U parameter?
Linear response theory
Density-functional perturbation theory (DFPT)
Sum over all q points in a q mesh

---
How to compute the Hubbard U parameter?
Using the HP (Hubbard Parameters) code of Quantum ESPRESSO
Input file “hp.FeO.in”:
Prefix and outdir must be exactly the same as in
the input file pw.FeO.scf.in
!
Size of the q point mesh: 1x1x1 in this case
U = 4.6 eV
Warning: This U value is not converged with respect to the k and q meshes!!!
Documentation: quantum-espresso/HP/Doc/INPUT_HP.txt
Theory:
I. Timrov, N. Marzari, M. Cococcioni, PRB 98, 085127 (2018)
I. Timrov, N. Marzari, M. Cococcioni, PRB 103, 045141 (2021)

---
DFT+U+V
Both U and V can be
computed using the
HP code
V.L. Campo Jr and M. Cococcioni, JPCM 22, 055602 (2010)
Theory:
I. Timrov, N. Marzari, M. Cococcioni, PRB 103, 045141 (2021)

---
Outline
Example 1: DFT+U study of FeO
Example 2: DFT with hybrid functionals: study of Si
Example 3: DFT with Van der Waals functionals: study of graphite

---
We need to setup the q mesh

---
Input file pw.Si.scf.in
Hybrid functionals are very computationally expensive!
SCF calculation
!
Override the functional written in the pseudo-
potential (PP) file.
Important: use a PP for the closest GGA (PBE
in this case), there are no PP's for hybrids.
!
Mesh for the q points 1x1x1 is the minimal
grid (q=0), it is fast but not very accurate
If .true. use extrapolation for the q->0 limit
Specifies that the singularity at q->0 is
analytically integrated

---
Popular hybrid functionals
input_dft = “pbe0”
J.P.Perdew, M. Ernzerhof, K.Burke, JCP 105, 9982 (1996)
C. Adamo, V. Barone, JCP 110, 6158 (1999)
input_dft = “b3lyp”
 P.J. Stephens,F.J. Devlin,C.F. Chabalowski,M.J. Frisch, J.Phys.Chem 98, 11623 (1994)
input_dft = “hse”
Heyd, Scuseria, Ernzerhof, J. Chem. Phys. 118, 8207 (2003)
Heyd, Scuseria, Ernzerhof, J. Chem. Phys. 124, 219906 (2006)

---
Types of treatement of divergences at q->0

---
Convergence of the total energy
wrt q point grid
Slow calculations do for scarce q meshes and check the “reference” folder

---
Outline
Example 1: DFT+U study of FeO
Example 2: DFT with hybrid functionals: study of Si
Example 3: DFT with Van der Waals functionals: study of graphite

---
Graphite
Graphite has Van der Waals (dispersive) interactions between layers.
The equilibrium inter-layer distance is too small with LDA, and too large with GGA
        with respect to the experimental value (3.336 A).
Van der Waals interactions must be taken into account.

---
Input file pw.graphite.vc-relax.in
Variable-cell optimization
Variable-cell optimization
!
!
Hexagonal lattice, a and c are in Angtrom!
Override the functional written in the PP file.
Important: use PP for the closest GGA (PBE in
this case), because there are no PP for non-
local functionals
If we do not specify anything inside these namelists,
then the default values will be used for various
control parameters
The k point grid is denser along xy than along z,
reflecting shorter periodicity in the xy plane

---
Types of the van der Waals correction

---
Structural optimization in graphite