QE-2021: Hands-on session – Day-6
TDDFPT
Iurii Timrov (EPFL, Switzerland)
Oscar Baseggio (SISSA, Italy)

---
Outline
1. Part I – Optical absorption in molecules
2. Part II – EELS in solids
(We will use HPC for this hands-on, because many examples are quite heavy)

---
Part I – Optical absorption in molecules
1. Example 1: turboDavidson – from the Independent Particle Approximation (IPA) to interacting electrons
2. Example 2: turboLanczos – total spectra at low cost for interacting electrons

---
turboDavidson program for calculations of absorption spectra
- The turbo_davidson.x program allows us to calculate absorption spectra of molecules using time-dependent density functional perturbation theory (TDDFpT).
- The interactions of electrons (Hartree and Exchange-Correlation effects) are taken into account fully ab initio and self-consistently (or they can be neglected if_dft_spectrum=.true.).
- The electronic transitions from occupied to empty states can be analyzed by selecting a frequency range in which the transitions occur.
- However, calculations of overall absorption spectra in a wide frequency range are computationally rather expensive, because many eigenvalues of the Hamiltonian must be computed.

---
turboDavidson program for calculations of absorption spectra
Coupled linear-response TDDFpT equations (resonant and anti-resonant):
These equations can be re-written as Casida's matrix equation:
interaction terms
where and
Davidson algorithm is used (the same algorithm as in the ground state SCF calculation) to solve the Casida's equations and to obtain the eigenvalues which are used for a calculation of the absorption coefficient.

---
Independent Particle Approximation
The simplest approximation: Independent Particle Approximation (IPA) - a sum of independent excitations from occupied to empty states.
Fermi's golden rule
The transition probability per unit time from occupied states to empty states reads:
is the external potential induced by the electric field.
and
are the eigenvalues
are the eigenvalues
and the eigenfunctions of the ground-state Kohn-Sham equation

---
Example 1: Input file for PWscf
Step 1. Perform a Self-Consistent Field ground-state calculation for benzene at the equilibrium structure using the pw.x program.
!
!
Specify the total number of Kohn-Sham bands
(occupied + some empty states)
Output
Input
pw.x < pw.benzene.scf.in > pw.benzene.scf.out

---
Example 1: Output file of PWscf
The output SCF file pw.benzene.scf.out :
HOMO
LUMO
HOMO – Highest Occupied Molecular Orbital
LUMO – Lowest Unoccupied Molecular Orbital
Energy gap = LUMO – HOMO = 5.1 (eV)

---
Example 1: Calculation of absorption spectra using turboDavidson (IPA)
Perform the turboDavidson calculation without the electronic interaction using the turbo_davidson.x program.
Same as in PWscf
!
This means we are using IPA
Obsolete variable for the IPA case
(will not be needed in future version of
QE for the IPA case)
turbo_davidson.x < turbo_davidson.benzene.in > turbo_davidson.benzene.out

---
Example 1: Post-processing step
Perform a spectrum calculation using the turbo_spectrum.x program
and using the eigenvalues computed in the previous step.
turbo_spectrum.benzene.in :
Prefix the same as in PWscf
Directory for temporary (same as in PWscf)
!
Type of previous calculation
Starting value of the freq. for the plot
End value of the freq. for the plot
Freq. step for the plot
Lorentzian broadening in Ry
File with Davidson eigenvalues
turbo_spectrum.x < turbo_spectrum.benzene.in > turbo_spectrum.benzene.out

---
Example 1: Calculation of absorption spectra in IPA
Absorption spectrum of benzene in the Independent Particle Approximation (file Benzene_spectrum.eps):
Use the script plot_spectrum.gp to produce this figure.
Energy gap = LUMO – HOMO = 5.1 (eV)

---
Example 1: Spectra including interactions
Perform the turboDavidson calculation without the electronic interaction using
the turbo_davidson.x program.
tmp
!
Switch on the interactions
.false.
0.004
turbo_davidson.x < turbo_davidson.benzene.in > turbo_davidson.benzene.out

---
Example 1: Comparison of spectra with and without
interactions
Interaction increases the gap and thus blue-shifts the peaks

---
turboLanczos program for calculation of absorption spectra
- The turbo_lanczos.x program allows us to calculate absorption spectra of molecules using time-dependent density functional perturbation theory (TDDFpT) without computing empty states!
- The interactions of electrons (Hartree and Exchange-Correlation effects) are taken into account fully ab initio and self-consistently.
- The electronic transitions from occupied to empty states cannot be analyzed (use turbo_davidson.x for this purpose).
- The overall absorption spectrum in a wide frequency range can be calculated at once!

---
turboLanczos program for calculation of absorption spectra
Coupled linear-response TDDFpT equations (resonant and anti-resonant):
perturbation
These equations can be re-written as a quantum Liouville equation:
interaction terms
Absorption coefficient is computed as:
Lanczos algorithm is used to solve recursively quantum Liouville equation in the standard batch representation. This allows us to avoid inversions and multiplications of large matrices.

---
Example 2: Calculation of absorption spectra using turboLanczos
Step 1. Perform a SCF ground-state calculation (no nbnd in the input):
pw.x < pw.benzene.scf.in > pw.benzene.scf.out
Step 2. Perform Lanczos recursions using the turbo_lanczos.x program.
!
tmp
turbo_lanczos.x < turbo_lanczos.benzene.in > turbo_lanczos.benzene.out

---
Example 2: Post-processing step
Perform a spectrum calculation using the post-processing program turbo_spectrum.x and using the Lanczos coefficients computed in the previous step.
!
1
turbo_spectrum.x < turbo_spectrum.benzene.in >... ...turbo_spectrum.benzene.out

---
Example 2: Post-processing step
No extrapolation of Lanczos coefficients
turbo_spectrum.benzene.in
turbo_lanczos.benzene.in
!
tmp
!
1
Must be equal !
You can use restart = .true. option in order not to start from scratch, when you want to increase the number of Lanczos iterations.

---
Example 2: Post-processing step
No extrapolation of Lanczos coefficients
No convergence yet even after
1500 iterations

---
Example 2: Lanczos coefficients
Behavior of Lanczos coefficients
Lanczos coefficients oscillate around half of the kinetic-energy cutoff (~30/2 = 15 Ry in this case). Hence, we can extrapolate these coefficients.

---
Example 2: Extrapolation of Lanczos coefficients
In the Liuoville-Lanczos approach, the absorption coefficient is computed as:
where is the tridiagonal matrix composed of the Lanczos coefficients.
Extrapolation

---
Example 2: Post-processing step
With extrapolation of Lanczos coefficients
turbo_spectrum.benzene.in
turbo_lanczos.benzene.in
!
!
tmp
1
Must be equal !
Must be equal !
Extrapolation until 20000
You can use restart = .true. option in order not to start from scratch, when you want to increase the number of Lanczos iterations.

---
Example 2: Post-processing step
With extrapolation of Lanczos coefficients
The spectrum is relatively well
converged after 1500 iterations
One Lanczos calculation to obtain spectrum in any wide frequency range!

---
Part II – EELS in solids
1. Example 3: EELS spectrum of Si using the turboEELS code (Lanczos algorithm)
2. Example 4: EELS spectrum of Si using the turboEELS code (Sternheimer algorithm)
OPTIONAL
(very slow)

---
Basic equations
Coupled (resonant and anti-resonant) frequency-dependent Sternheimer equations:
perturbation
interaction terms
These equations can be re-written as a quantum Liouville equation and solved using the Lanczos algorithm:
Susceptibility
Loss function

---
Example 3
Coupled (resonant and anti-resonant) frequency-dependent Sternheimer equations:
Let's use the Lanczos algorithm
perturbation
interaction terms
These equations can be re-written as a quantum Liouville equation and solved using the Lanczos algorithm:
Susceptibility
Loss function

---
Example 3: Input file for PWscf
Step 1. Perform a Self-Consistent Field ground-state calculation for silicon using the pw.x program.
!
!
Input
Output
pw.x < pw.si.scf.in > pw.si.scf.out

---
Example 3 : Input file for turboEELS
Step 2. Perform Lanczos recursions using the turbo_eels.x program in order to compute Lanczos coefficients, which will be needed in Step 3.
Same as in the PWscf input
!
Restart keywords
Type of the algorithm that is used
Number of Lanczos iterations
Components of the transferred momentum q
How to specify q1, q2, q3 ? -> See next slide
turbo_eels.x < turbo_eels.si.lanczos.in > turbo_eels.si.lanczos.out

---
Example 3: Transferred momentum specification
- lattice parameter
Example: and .
Therefore, we obtain:

---
Example 3: Post-processing step
Step 3. Perform a spectrum calculation using the post-processing program turbo_spectrum.x and using the Lanczos coefficients computed in the previous step.
!
turbo_spectrum.x < turbo_spectrum.si.in > turbo_spectrum.si.out

---
Example 3: Computed quantities
The code turbo_spectrum.x produces a file silicon.plot_eps.dat which contains the real and imaginary parts of the dielectric function and its inverse:

---
Example 3: The computed EELS
No extrapolation of Lanczos coefficients
The spectrum (loss function)
is not converged after 500
iterations with no extrapolation
Here, k points mesh 10x10x10 1 1 1 is used.

---
Example 3: Convergence of EELS
No extrapolation of Lanczos coefficients
Here, k points mesh 10x10x10 1 1 1 is used.

---
Example 3: Post-processing step
Step 3. Perform a spectrum calculation using the post-processing program turbo_spectrum.x and using the Lanczos coefficients computed in the previous step.
!
20000
'osc'
turbo_spectrum.x < turbo_spectrum.si.in > turbo_spectrum.si.out

---
Example 3: Convergence of EELS
With extrapolation of Lanczos coefficients
Here, k points mesh 10x10x10 1 1 1 was used.

---
Example 3: Where is the plasmon peak?
Modify the script plot_spectrum.gp and use the file silicon.plot_eps.dat to plot this figure
plasmon

---
Example 4
Coupled (resonant and anti-resonant) frequency-dependent Sternheimer equations:
perturbation
interaction terms
These equations can be re-written as a quantum Liouville equation and solved using the Lanczos algorithm:
Let's use the Sternheimer
algorithm
Susceptibility
Loss function

---
Example 4
The implementation of the Sternheimer algorithm in turboEELS is very recent.
This algorithm is not fully optimized, therefore the calculation is much slower than
in the previous examples.
We will need to use HPC for this exercise.
Moreover, the disc space must be enough, because the code writes quite large
files on disc and it may fail if there is not enough space.
Use the parallelization of k point pools to speed up the calculation.

---
Example 4 : Input file for turboEELS
Step 1. Perform a SCF ground-state calculation for Si.
Step 2. Solve the Sternheimer equations using turbo_eels.x
Same as in the PWscf input
!
Type of the algorithm that is used
Components of the transferred momentum q
The value of Lorenzian broadening in Ry
The units (0 → Ry, 1 → eV)
Keywords that control the range in which the
spectrum is plotted
turbo_eels.x < turbo_eels.si.sternheimer.in > ...
...turbo_eels.si.sternheimer.out

---
Example 4: The computed EELS
The Sternheimer and Lanczos algorithms give exactly the same spectrum.
Sternheimer is much slower than Lanczos!

---
Example 4: Convergence w.r.t. k mesh
Convergence of EELS with respect to the size of the k points mesh

---
Example 4: Plasmon dispersion
Plasmon dispersion in bulk silicon
By increasing q, the plasmon peak blue-shifts and broadens, because it enters in the electron-hole continuum.

---
Example 4: Plasmon dispersion and e-h continuum
The excitation region of the electron gas in (q,w) space
The plasmon line becomes strongly damped in a region of electron-hole pairs.
G. D. Mahan, Many-Particle Physics, Plenum Press, 2nd ed. New York, (1975)